## Slide 1: THERMO-MECHANICAL MODEL TO STUDY MICROSTRUCTURE DURING ADDITIVE MANUFACTURING
Nikhil Mohanan
MSc. Mechanics and Mathematical Modeling
Higher School of Theoretical Mechanics
Peter the Great St. Petersburg Polytechnic University
Internal Supervisor: Prof. Vitaly A Kuzkin
Higher School of Theoretical Mechanics
Peter the Great St. Petersburg Polytechnic University, Russia
External Supervisor: Prof. Manas V Upadhyay
Laboratoire de Mecanique des Solides
Ecole Polytechnique, Paris, France

## Slide 2: Motivation : What happens to a microstructure during AM?
Source: Manas V Upadhyay, 2020 (hal-02439503v3)
BeAM Additive Manufacturing, LMS

## Slide 3: Aim, Objectives and Methodology
Aim :
Study microstructure evolution due to SSTC during AM
Objectives :
Create a finite element micromechanical solver to study SSTC on the microstructure during AM:
    To account for the effects of fully coupled Thermo-Elastodynamics
    To account for heterogeneous material behavior
Methodology :
    Divide and Conquer Methodology - Model individual components and combine

## Slide 4: Linear ElastoStatics (ES)
Governing Equation
Constitutive Laws
𝝈 = ℂ
Definition of Strains
The Kirsch Problem (Kulesh,2001)
Initial Condition
Boundary Condition
Chart: Y (mm)
| 0.100987535360441 | 0.120915885888392 | 0.13228774987820699 | 0.13650004979396099 | 0.144965023107089 | 0.15487536706223701 | 0.16478840258282601 | 0.17325606746139599 | 0.18600062982631299 | 0.2044351615343 | 0.218606253583147 | 0.23990999405164001 | 0.261246033305431 | 0.28825858407508398 | 0.32669952170882099 | 0.37370502057701799 | 0.43071237662536899 | 0.48630666081699803 | 0.54333554938887996 | 0.59465831922504497 | 0.64884491469083405 | 0.71587566044286999 | 0.77435799435309605 | 0.83141379857939202 | 0.91842134303732403 | 0.99402472472014503
Analytical | 0.0058542 | 0.03608 | 0.064404 | 0.11158 | 0.17764 | 0.23048 | 0.28145 | 0.34561 | 0.41167 | 0.48907 | 0.55513 | 0.62121 | 0.66465 | 0.72885 | 0.78175 | 0.8309 | 0.86874 | 0.89715 | 0.9199 | 0.94263 | 0.95783 | 0.96928 | 0.97316 | 0.97704 | 0.98475 | 0.98678
L = 1.0
R = 0.1
X
Y
TS = 1.0
X
Y
Plot of vs length

## Slide 5: Linear ElastoDynamics (ED)
Governing Equation
Constitutive Laws
𝝈 = ℂ
Definition of Strains
1D-Rod Wave Propagation (Eran,2007)
Initial Condition
Boundary Condition:
Chart: 𝒙 /𝑳
Plot of vs at time over the length

## Slide 6: Heat Conduction
Governing Equation
Fourier Law
1st and 2nd Danilovskaya Problem (Nickel-Sackman, 1968)
Initial Condition Boundary Condition
Plot of (K) vs at
Chart: t (s)
| 0 | 2.0660462928750001E-3 | 7.1774112271978996E-2 | 0.15191319246145099 | 0.20551281620586601 | 0.26746061074344102 | 0.31906137669230999 | 0.376843484395471 | 0.44702186985588099 | 0.51720025531628999 | 0.57498236301945105 | 0.64102865589411095 | 0.70292605905868899 | 0.76482346222326703 | 0.82460442772197395 | 0.89473242180938595 | 0.96889172573655402 | 1.03073873752814 | 1.09871669970101 | 1.1419692948567199 | 1.2058319615681801 | 1.26143044310814 | 1.3170289246481 | 1.3767259045251501 | 1.44673631874223 | 1.50231800315786 | 1.5702119797090699 | 1.6586992306917101 | 1.7348237981657499 | 1.80684986730272 | 1.8685289078509799 | 1.93229079181644 | 2.0124802633789098
Analytical H = 0.5 | 0 | 0.0012228 | 0.0020996 | 0.0074932 | 0.015324 | 0.02685 | 0.035909 | 0.045792 | 0.058145 | 0.070498 | 0.080381 | 0.091911 | 0.10221 | 0.1125 | 0.12116 | 0.13228 | 0.14177 | 0.15084 | 0.1595 | 0.16486 | 0.17311 | 0.17971 | 0.18632 | 0.19292 | 0.20118 | 0.20737 | 0.21398 | 0.22307 | 0.23051 | 0.23795 | 0.24292 | 0.24871 | 0.25533
Analytical H = 5.0 | 0 | 0.0031792 | 0.014573 | 0.026974 | 0.044507 | 0.071299 | 0.10531 | 0.13211 | 0.15272 | 0.17129 | 0.18779 | 0.20636 | 0.22699 | 0.24764 | 0.26622 | 0.28584 | 0.30443 | 0.31993 | 0.33337 | 0.34784 | 0.3613 | 0.37372 | 0.38615 | 0.39754 | 0.40792 | 0.41828 | 0.42866 | 0.43903 | 0.44734 | 0.45462 | 0.46293 | 0.47229 | 0.48063 | 0.48896 | 0.49834 | 0.50563 | 0.51294 | 0.52025 | 0.52757 | 0.53592 | 0.54219 | 0.54743 | 0.55266 | 0.55582
Chart: t (s)
| 0 | 2.4271541297744E-2 | 5.3856483309124001E-2 | 8.3398747403125001E-2 | 0.10246663120335001 | 0.123275164348087 | 0.142336951302972 | 0.161398738257857 | 0.185658085864921 | 0.202997514011313 | 0.23419507161507 | 0.26018897172130701 | 0.30005929182093 | 0.33821944680273802 | 0.37987309416425202 | 0.41977999533591298 | 0.46492103823179298 | 0.50136493125044801 | 0.53436410665211598 | 0.57430758889581601 | 0.60557221179831 | 0.64205878273434402 | 0.67855145051571697 | 0.71851322329543699 | 0.75848718976583596 | 0.80194245492526095 | 0.84365707074017304 | 0.89580948577682196 | 0.951443199502498 | 1.0036017113844899 | 1.0557724169571601 | 1.10619637633997 | 1.1496821257261001 | 1.19664307695591 | 1.25577028306129 | 1.3148913923213299 | 1.3774998971157399 | 1.44360799113519 | 1.51493193634284 | 1.59495912827305 | 1.6697643721697299 | 1.7497976609452901 | 1.8159057549647399 | 1.88724189386307 | 1.9533560847278599 | 2.0090385732162499
Analytical | 0 | 0.0036522 | 0.0048599 | 0.014649 | 0.030574 | 0.046499 | 0.06365 | 0.080801 | 0.10285 | 0.11633 | 0.14328 | 0.16655 | 0.19963 | 0.22658 | 0.25107 | 0.27679 | 0.30005 | 0.3221 | 0.33679 | 0.35515 | 0.36862 | 0.38208 | 0.39432 | 0.40901 | 0.42124 | 0.43347 | 0.44571 | 0.45916 | 0.47261 | 0.48484 | 0.49461 | 0.50562 | 0.51172 | 0.51905 | 0.53004 | 0.54227 | 0.55326 | 0.56058 | 0.56911 | 0.57765 | 0.58618 | 0.59349 | 0.6008 | 0.60689 | 0.61298 | 0.61662

## Slide 7: Thermo-ElastoDynamics (T-ED)
Plot of u(mm) and (K) vs at
Definition of Strains
Governing Equation
Constitutive Laws
Fully Coupled Second Danilovskaya Problem (Sternberg,1958)
Initial Condition: Boundary Condition:
Chart: t (s)
Exact δ = 1.00,H = 0.5 | 0 | 0.0017047 | 0.0062631 | 0.013284 | 0.021524 | 0.03141 | 0.038831 | 0.046251 | 0.053673 | 0.059861 | 0.065642 | 0.070187 | 0.074326 | 0.077643 | 0.080552 | 0.083056 | 0.084324 | 0.085182 | 0.086046 | 0.086073 | 0.087325 | 0.08941 | 0.091901 | 0.095219 | 0.09895 | 0.1031 | 0.10683 | 0.11056 | 0.11429 | 0.11719 | 0.12092 | 0.12383 | 0.12715 | 0.13047 | 0.13461 | 0.13752 | 0.14125 | 0.14498 | 0.14871 | 0.15161 | 0.15328
Exact δ = 0.36,H = 0.5 | 0 | 0.0017047 | 0.0062631 | 0.014095 | 0.025219 | 0.03469 | 0.042927 | 0.050341 | 0.05858 | 0.066823 | 0.074652 | 0.081657 | 0.088668 | 0.094856 | 0.10105 | 0.106 | 0.11055 | 0.11469 | 0.11842 | 0.12297 | 0.12752 | 0.13207 | 0.13703 | 0.14199 | 0.14653 | 0.1519 | 0.15687 | 0.161 | 0.16514 | 0.16969 | 0.17424 | 0.17838 | 0.18252 | 0.18707 | 0.19121 | 0.19535 | 0.19907 | 0.2028 | 0.20653 | 0.20901
Exact δ = 0.00,H = 0.5 | 0 | 0.0017047 | 0.0062631 | 0.014095 | 0.023976 | 0.037974 | 0.047855 | 0.059794 | 0.070087 | 0.07956 | 0.089441 | 0.099739 | 0.10962 | 0.11786 | 0.12528 | 0.13476 | 0.14342 | 0.15125 | 0.15867 | 0.16568 | 0.1727 | 0.17889 | 0.18508 | 0.1925 | 0.19952 | 0.20572 | 0.21274 | 0.21893 | 0.22472 | 0.23009 | 0.23547 | 0.24084 | 0.24622 | 0.25036 | 0.25532
Exact δ = 1.00,H = 5.0 | 0 | 0.0031792 | 0.014573 | 0.026974 | 0.044507 | 0.071299 | 0.10531 | 0.12594 | 0.15378 | 0.17029 | 0.18887 | 0.20849 | 0.22606 | 0.24055 | 0.25092 | 0.25923 | 0.26346 | 0.2646 | 0.26368 | 0.26065 | 0.25865 | 0.25564 | 0.25059 | 0.24653 | 0.24348 | 0.24456 | 0.2477 | 0.25187 | 0.25914 | 0.26951 | 0.2799 | 0.28925 | 0.29654 | 0.30485 | 0.31317 | 0.3215 | 0.32776 | 0.33713 | 0.34338 | 0.35067 | 0.35796 | 0.36527 | 0.37152 | 0.3778 | 0.38406 | 0.39136 | 0.39555
Exact δ = 0.36,H = 5.0 | 0 | 0.0031792 | 0.014573 | 0.026974 | 0.044507 | 0.071299 | 0.10531 | 0.12902 | 0.15377 | 0.1713 | 0.194 | 0.2167 | 0.23735 | 0.24767 | 0.26213 | 0.27661 | 0.29007 | 0.30147 | 0.31185 | 0.31914 | 0.32541 | 0.32963 | 0.33282 | 0.337 | 0.33805 | 0.34116 | 0.34842 | 0.35984 | 0.36815 | 0.37646 | 0.38582 | 0.39518 | 0.4035 | 0.41182 | 0.41912 | 0.42538 | 0.43269 | 0.43997 | 0.44727 | 0.45251 | 0.4598 | 0.4671 | 0.47233 | 0.4786 | 0.48279 | 0.48698
Exact δ = 0.00,H = 5.0 | 0 | 0.0031792 | 0.014573 | 0.026974 | 0.044507 | 0.071299 | 0.10531 | 0.13211 | 0.15272 | 0.17129 | 0.18779 | 0.20636 | 0.22699 | 0.24764 | 0.26622 | 0.28584 | 0.30443 | 0.31993 | 0.33337 | 0.34784 | 0.3613 | 0.37372 | 0.38615 | 0.39754 | 0.40792 | 0.41828 | 0.42866 | 0.43903 | 0.44734 | 0.45462 | 0.46293 | 0.47229 | 0.48063 | 0.48896 | 0.49834 | 0.50563 | 0.51294 | 0.52025 | 0.52757 | 0.53592 | 0.54219 | 0.54743 | 0.55266 | 0.55582
Chart: t (s)
Analytical δ = 1.00,H = 0.5 | 0 | 0.00054436 | 0.0020094 | 0.0038837 | 0.0052361 | 0.0070031 | 0.0088727 | 0.011054 | 0.013442 | 0.015518 | 0.017179 | 0.019982 | 0.022058 | 0.024133 | 0.026312 | 0.02818 | 0.030567 | 0.032642 | 0.034097 | 0.035241 | 0.035661 | 0.035459 | 0.034843 | 0.033915 | 0.032883 | 0.031541 | 0.030095 | 0.028443 | 0.026582 | 0.024618 | 0.022551 | 0.02007 | 0.017795 | 0.015416 | 0.013141 | 0.010556 | 0.0078669 | 0.005385 | 0.0042476
Analytical δ = 0.36,H = 0.5 | 0 | 0.00054436 | 0.0023205 | 0.0042982 | 0.0064807 | 0.0084543 | 0.010739 | 0.013438 | 0.015722 | 0.017589 | 0.019769 | 0.021533 | 0.0234 | 0.025475 | 0.02755 | 0.029417 | 0.031595 | 0.033774 | 0.037611 | 0.040516 | 0.042279 | 0.044458 | 0.0456 | 0.046847 | 0.047681 | 0.047788 | 0.047585 | 0.047071 | 0.046039 | 0.043972 | 0.042215 | 0.040148 | 0.038493 | 0.035804 | 0.03446 | 0.032288 | 0.030115 | 0.027219 | 0.024218 | 0.022252 | 0.019562 | 0.016975 | 0.013353 | 0.0098347 | 0.0075579 | 0.005385 | 0.0035222
Analytical δ = 1.00,H = 5.0 | 0 | 0.00075799 | 0.0031428 | 0.0055449 | 0.0087559 | 0.012783 | 0.018027 | 0.022867 | 0.02892 | 0.032958 | 0.039016 | 0.046691 | 0.054771 | 0.064468 | 0.075785 | 0.082656 | 0.089527 | 0.097206 | 0.1057 | 0.11459 | 0.11823 | 0.12146 | 0.12266 | 0.12225 | 0.12103 | 0.119 | 0.11615 | 0.11412 | 0.11127 | 0.10802 | 0.10153 | 0.095441 | 0.092599 | 0.087324 | 0.083671 | 0.078395 | 0.075147 | 0.069872 | 0.063783 | 0.060131 | 0.052016 | 0.043901 | 0.03619 | 0.026857 | 0.0081925 | -0.0011415 | -0.011691 | -0.01859 | -0.027109 | -0.033196
Analytical δ = 0.36,H = 5.0 | 0 | 0.00075799 | 0.0031428 | 0.0055449 | 0.0083567 | 0.011982 | 0.016013 | 0.019644 | 0.024485 | 0.032157 | 0.03862 | 0.043873 | 0.051146 | 0.057209 | 0.064079 | 0.070952 | 0.077824 | 0.083484 | 0.090761 | 0.097231 | 0.1041 | 0.11057 | 0.11826 | 0.12432 | 0.1312 | 0.1405 | 0.14535 | 0.1498 | 0.15223 | 0.15384 | 0.15424 | 0.15342 | 0.1518 | 0.14936 | 0.14449 | 0.13921 | 0.13475 | 0.12947 | 0.12339 | 0.11527 | 0.10675 | 0.10027 | 0.093776 | 0.086475 | 0.07877 | 0.071063 | 0.059301 | 0.049974 | 0.040239 | 0.034156 | 0.0053601 | -0.0072111 | -0.018163 | -0.025463 | -0.035197 | -0.044524 | -0.048987
Analytical δ = 0.00,H = 5.0 | 0 | 0.00075799 | 0.003151 | 0.0051491 | 0.0083617 | 0.012791 | 0.017631 | 0.024492 | 0.033374 | 0.043071 | 0.053982 | 0.063279 | 0.072577 | 0.081876 | 0.093198 | 0.10209 | 0.11059 | 0.1207 | 0.1304 | 0.14132 | 0.15305 | 0.16357 | 0.17166 | 0.17449 | 0.1761 | 0.1761 | 0.17366 | 0.17 | 0.16392 | 0.15743 | 0.15134 | 0.14445 | 0.13836 | 0.13106 | 0.12376 | 0.11525 | 0.1043 | 0.095784 | 0.088079 | 0.077942 | 0.069427 | 0.059695 | 0.051991 | 0.043071 | 0.036178 | 0.027258 | 0.011851 | 0.00090334 | -0.0088281 | -0.017343 | -0.024642 | -0.033562 | -0.042887 | -0.050998 | -0.058702
= 0.36, h = 5.0
= 0.00, h = 5.0
= 1.00, h = 5.0
= 1.00, h = 0.5
= 0.36, h = 0.5
= 0.00, h = 0.5

## Slide 8
Homogenization Problem
(EVP FFT, Lebonsohn,2012)
Governing Equation
Constitutive Laws:
Boundary Condition:
=
Chart: X (mm)
| 0 | 6.25E-2 | 0.125 | 0.1875 | 0.25 | 0.3125 | 0.375 | 0.4375 | 0.5 | 0.5625 | 0.625 | 0.6875 | 0.75 | 0.8125 | 0.875 | 0.9375 | 1
𝝈11 FEM | 2.906 | 2.628 | 2.3017 | 3.1279 | 2.892 | 2.5066 | 2.4237 | 2.6818 | 2.688 | 2.682 | 2.7448 | 2.9231 | 2.9653 | 2.8865 | 2.8433 | 2.8749 | 2.712
𝝈22 FEM | 0.35914 | 1.3233 | 1.1733 | 1.5585 | 1.4388 | 1.4934 | 1.3071 | 1.246 | 1.0029 | 0.94815 | 0.87895 | 1.4325 | 1.057 | 0.75768 | 0.69853 | 0.91916 | 0.76831
𝝈33 FEM | 1.3082 | 1.8727 | 1.3486 | 1.566 | 1.4389 | 1.3215 | 1.0527 | 1.488 | 1.3485 | 1.1171 | 0.50915 | 1.0215 | 1.0334 | 1.0173 | 1.1365 | 1.6414 | 1.7526
𝝈11 EVP | 2.5149 | 2.5566 | 2.643 | 2.498 | 2.7289 | 3.017 | 3.0097 | 2.93 | 2.7612 | 2.63 | 2.5561 | 2.5983 | 2.5841 | 2.6549 | 2.7083 | 2.6704 | 2.6238 | 2.5695 | 2.4963 | 2.5774 | 2.7593 | 2.8298 | 2.9826 | 3.0425 | 2.9817 | 2.9475 | 2.8855 | 2.8408 | 2.7835 | 2.7389 | 2.6971 | 2.6147
𝝈22 EVP | 0.65132 | 1.1491 | 1.3179 | 1.1799 | 1.2043 | 1.4635 | 1.5185 | 1.4223 | 1.3177 | 1.3253 | 1.3858 | 1.5401 | 1.5667 | 0.9783 | 1.0338 | 1.0378 | 0.99252 | 0.91088 | 0.83712 | 1.0177 | 1.361 | 1.3235 | 1.3972 | 1.0821 | 0.75942 | 0.74646 | 0.74938 | 0.84026 | 0.80778 | 0.79203 | 0.67107 | 0.76324
𝝈33 EVP | 1.3785 | 1.4998 | 1.6642 | 1.3863 | 1.4075 | 1.4369 | 1.4756 | 1.406 | 1.3715 | 1.2782 | 1.2039 | 1.1905 | 1.2354 | 1.4055 | 1.4624 | 1.3351 | 1.2898 | 1.1676 | 1.0034 | 0.73925 | 0.73298 | 0.6518 | 0.91664 | 1.3063 | 1.1549 | 0.98167 | 0.96133 | 0.94674 | 0.99425 | 1.5845 | 1.5201 | 1.4551
Chart: X (mm)
| 0 | 6.25E-2 | 0.125 | 0.1875 | 0.25 | 0.3125 | 0.375 | 0.4375 | 0.5 | 0.5625 | 0.625 | 0.6875 | 0.75 | 0.8125 | 0.875 | 0.9375 | 1
ε11 FEM | 7.8552e-06 | 1.2109e-05 | 1.3187e-05 | 1.1015e-05 | 1.1745e-05 | 1.093e-05 | 9.4286e-06 | 8.5655e-06 | 8.4546e-06 | 8.5753e-06 | 1.0139e-05 | 1.1827e-05 | 9.7325e-06 | 7.7618e-06 | 8.7716e-06 | 9.2167e-06 | 9.2293e-06
ε22 FEM | 9.5662e-07 | 2.0586e-07 | -2.1091e-06 | 8.6104e-07 | -4.9823e-07 | -7.4273e-08 | 5.0837e-07 | 1.4452e-06 | 1.5914e-06 | 1.8272e-06 | 5.4434e-07 | -1.4447e-06 | -4.4411e-07 | 2.9051e-07 | -5.0823e-07 | 1.0901e-06 | 9.5662e-07
ε33 FEM | 7.1597e-07 | -1.8115e-07 | -1.0285e-06 | 1.1495e-06 | 7.7397e-07 | 2.3098e-07 | 2.8691e-08 | 1.2722e-06 | 4.5263e-07 | -5.1235e-07 | -2.0733e-06 | 8.1983e-07 | 1.2443e-06 | 1.6591e-06 | 1.4832e-06 | 1.017e-06 | 7.1597e-07
ε11 EVP | 8.2986e-06 | 1.1233e-05 | 1.3308e-05 | 1.3648e-05 | 1.2178e-05 | 1.1554e-05 | 1.1255e-05 | 1.1178e-05 | 1.058e-05 | 1.0755e-05 | 1.0898e-05 | 1.0888e-05 | 1.0423e-05 | 8.0403e-06 | 8.3452e-06 | 8.4764e-06 | 8.4219e-06 | 8.3542e-06 | 8.2474e-06 | 9.4727e-06 | 1.1202e-05 | 1.1434e-05 | 1.163e-05 | 1.0263e-05 | 8.7229e-06 | 8.8443e-06 | 8.6074e-06 | 8.4086e-06 | 8.1322e-06 | 9.3133e-06 | 9.194e-06 | 8.6949e-06
ε22 EVP | 2.5006e-07 | -8.7793e-07 | -1.7786e-06 | -1.9261e-06 | -1.1818e-06 | -4.1952e-07 | 1.9724e-07 | -1.7805e-07 | -2.4689e-07 | -7.1427e-07 | -9.1234e-07 | -1.7768e-07 | 2.5182e-07 | 1.1532e-06 | 1.4483e-06 | 1.6874e-06 | 1.6283e-06 | 1.4438e-06 | 1.3829e-06 | 5.9929e-07 | -1.2567e-06 | -1.1846e-06 | -1.4144e-06 | -2.5226e-07 | -1.7221e-07 | -3.9463e-07 | -3.179e-07 | 1.3952e-07 | 2.168e-07 | 5.9008e-07 | 2.8304e-07 | 7.2075e-07
ε33 EVP | 9.2155e-07 | 4.9266e-07 | 1.9273e-07 | -1.1697e-06 | 1.3236e-07 | 1.1946e-06 | 1.0562e-06 | 9.9667e-07 | 1.022e-06 | 8.6383e-07 | 7.3537e-07 | 3.9196e-07 | 5.4794e-07 | 1.3033e-06 | 1.0489e-06 | 3.4225e-07 | 1.7097e-07 | -1.1493e-07 | -5.9507e-07 | -1.0401e-06 | 1.6721e-07 | -2.3708e-07 | 8.1969e-07 | 1.3043e-06 | 1.6508e-06 | 1.292e-06 | 1.2863e-06 | 1.093e-06 | 1.2041e-06 | 7.5415e-07 | 7.072e-07 | 6.5379e-07
EBSD Image of Microstructure
Euler Angle
Representation
Stress Field
Calculation
Heterogeneous Elasticity
Plot of (Mpa) and vs

## Slide 9: Application Problem : FEM-AM
Transient Displacement Contour over complete domain
Transient Temperature Contour over complete domain
Source: MVU Research Group LMS

## Slide 10: Solution to Application Problem
Chart: t (s)
Chart: t (s)
Chart: t (s)
Plot of (K) vs at
Plot of (Mpa) and vs at

## Slide 11: Summary and Perspectives
We have developed a Thermo-Elastodynamic numerical model for anisotropic polycrystalline materials to study solid state thermal cyclic response during metal AM.
Future Perspectives for PhD Research:
  Addition of VOCE Hardening Law
  Addition of Phenomenological Plasticity Models
  Addition of Phase Transformation Models
  Addition of Crystal Plasticity Models
  Create a Dislocation Dynamics Model for this simulation

## Slide 12
End of Presentation